## Slide 1: Adaptive phase-field modeling of heterogeneous materials
Treball de final de grau
Roger Llorenç i Vilanova
Director: Antonio Rodriguez-Ferran
Departament d’Enginyeria Civil i Ambiental

## Slide 2: Fracture
Understanding cracks: avoid, stop, mitigate, promote and control
Homogeneous / heterogeneous materials
Failure / Success

## Slide 3: Computational fracture mechanics
Discontinuous models: sharp cracks
Discontinuous displacement field
Might be less efficient due to remeshing

## Slide 4: Computational fracture mechanics
Continuous models – phase field: diffuse cracks
Continuous displacement field
Loss of stiffness represented by damage variable d
d = 0 for intact material; d = 1 for fully broken material
Length-scale parameter l
History variable H

## Slide 5: Energy minimization principle
Continuous models – phase field:
Based on an energy minimization principle
Francfort and Marigo (1998)

## Slide 6: Regularization of the fracture energy
Continuous models – phase field:
Regularization of the fracture energy – Tractable numerically!
Bourdin et al., (2000)

## Slide 7: Continuous displacement field
Two-dimensional tension test

## Slide 8: Continuous displacement field
Damage field and deformed mesh
Deformation scale factor = 10

## Slide 9: Adaptive refinement
Fine meshes required along the crack  High computational cost
Refinement value d > d* = 0.2  Automatic refinement
Refinement factor m = 10
m
m
m
m

## Slide 10: Adaptive refinement example

## Slide 11: Adaptive refinement example

## Slide 12: Adaptive refinement example
Deformation scale factor = 10

## Slide 13: Goals
Acquire familiarity with the existing adaptive phase-field model for homogeneous materials (Muixí, 2020)
Extend the phase-field model and the Matlab code to heterogeneous materials
Design and carry out computational tests of fracture in heterogeneous materials
Analyze the results and gain insight of fracture in heterogeneous materials

## Slide 14: Arrest, deflection and penetration of the crack
Fracture toughness
Young modulus E = 210 GPa
Poisson’s ratio ν = 0

## Slide 15: Arrest, deflection and penetration of the crack

## Slide 16: Arrest, deflection and penetration of the crack

## Slide 17: Arrest, deflection and penetration of the crack

## Slide 18: Arrest, deflection and penetration of the crack

## Slide 19: Arrest, deflection and penetration of the crack
Shear test

## Slide 20: Arrest, deflection and penetration of the crack

## Slide 21: Arrest, deflection and penetration of the crack

## Slide 22: Arrest, deflection and penetration of the crack

## Slide 23: Arrest, deflection and penetration of the crack

## Slide 24: Improving the resistance by placing inclusions

## Slide 25: Improving the resistance by placing inclusions

## Slide 26: Improving the resistance by placing inclusions

## Slide 27: Improving the resistance by placing inclusions

## Slide 28: My contributions
Extended the adaptive hybrid phase-field model implementation for homogeneous materials, Muixí (2020), to heterogeneous materials
Developed a robust algorithm for visualizing different sorts of deformed meshes during runtime
Design, execution and analysis of experiments using a variety of tools (Matlab, ez4u, LaCàN computer cluster, NotePad++ and Excel)

## Slide 29: Conclusions
Qualitative analysis of fracture’s behavior when encountering heterogeneity: crack arrest, deflection, penetration and nucleation
Increasing the GcRatio does not always result in a higher peak force & total displacement
Obtaining the maximum peak force or total displacement by distributing a constant area into different inclusions
Fracture can be narrowly guided by offering paths of less resistance

## Slide 30: Outlook
Probabilistic inclusions
Extension to three-dimensions
Experimental validation – Design of multi-layered materials

## Slide 31: Adaptive hybrid phase-field model
Ambati et al. (2015)

## Slide 32: Validation
Statement;
Ambati et al. (2015)
Experiment with cement mortar – Area marking the observed crack patterns; Ambati et al. (2015)
Hybrid phase-field model; Ambati et al. (2015)
Adaptive hybrid phase-field model; Muixí (2020)

## Slide 33: Computational fracture mechanics
Continuous displacement field
Deformation scale factor = 10

## Slide 34: Adaptive refinement

## Slide 35: Adaptive refinement
Deformation scale factor = 10

## Slide 36: Material parameters and heterogeneity
Young modulus E = 210 GPa
Poisson’s ratio ν = 0
Fracture toughness

## Slide 37: Arrest, deflection and penetration of the crack
Tension test

## Slide 38: Improving the resistance by placing inclusions
Crack nucleation
Breaks symmetry

## Slide 39: Improving the resistance by placing inclusions